# HOW TO USE THIS ARCHITECTURAL MATERIAL SPECIFICATION:

This is an “edit-out” document with specification language for several project options. Select appropriate text based on the project requirements and delete (edit-out) all other text. Locations where language for Project-specific requirements is to be inserted, deleted, and/or selected are indicated like this: [select text].

# PRODUCT

## ROPPE PIXELART DIGITALLY PRINTED FLOORING, MINIMALIST COLLECTION

## Roppe PixelArt Digitally Printed Flooring, Minimalist Collection shown in the finish schedule or listed herein as Roppe PixelArt shall be 19 11/16” (50 cm) square in nominal size and 1/8” (3.2 mm) in nominal thickness, furnished by the Roppe Corporation of Fostoria, Ohio. PixelArt with DiamondShield Pro Satin Finish with a Subtle Emboss shall have a current FloorScore Certification and not contain Recycled Materials. Roppe PixelArt shall be in the color [3000 Monochrome] [3001 Elemental] [3002 Refined] [3003 Unadorned] [3004 Nuanced] [3005 Serene] [3006 Muted] [3007 Austere] [3008 Understated] [3009 Subtle] [3010 Stark] [3011 Whisper] [3012 Streamlined] [3013 Crisp] [3014 Delicate] [3015 Tranquil] [3016 Essential] [3017 Restrained] [3018 Neutral] [3019 Bare] [3020 Pure] from the Minimalist pattern as selected.

# WARRANTY

20 Year Limited Commercial Warranty

# ATTRIBUTES, CERTIFICATIONS, & REGULATORY INFORMATION

- Manufactured in Fostoria, Ohio

- Contributes to LEED v5 Requirements

- Achieved NSF/ANSI 332 Level 1 Certification

- Achieved FloorScore Certification

- Achieved GreenGuard Gold Certification

- Meets California Department of Public Health V1.2 (CA Section 01350) requirements

- Meets Collaborative for High Performance Schools (CHPS) requirements

- Does Not Contain Recycled Materials

- Red List Chemical Free

- Recyclable Through the Roppe Impact Program

- Qualifies for American Made Products Acts and/or Requirements

Roppe Corporation  |  1600 North Union Street  |  Fostoria, Ohio 44830 U.S.A.

phone: (800) 537-9527  |  e-mail: sales@roppe.com  |  website: www.roppe.com

This document is provided to assist in the preparation of a Project or Master Specification that has been formatted in accordance with the Construction Specifications Institute (CSI)’s MasterFormat®. Ensure the latest publicized version of all product information is utilized for this specification, Roppe will not be liable for any damages arising out of the misuse of any information or specifications found in this document.

The contents contained within this Architectural Material Specification (AMS) may be utilized or copied into another projected related document, but this original document will remain in effect at the time of product installation, this AMS shall not be supplemented or replaced by the resulting project documentation. Any alterations to the wording or requirements contained in or derived from this document shall void all related warranties.